## Slide 1: SPINE Meeting 2016 Secondary electron emission model effect on the electrostatic equilbrium in GEO
Pierre Sarrailh
Mohamed Belhaj
Denis Payan

## Slide 2: Overview
CNES R&T 2015 « Charging and electrostatic risks »
TO: Denis Payan (CNES)
Scope
  Surface charging (eclipse or not) greatly influenced by the secondary emission yield
  Actual SPIS (and NASCAP) models well fitted at normal incidence but angular model discrepancies wrt experiments (model efficient for very high energy >> 10 keV)
  Measurement for incidence angle > 70° very difficult on dielectrics  need to extrapolate using models
Objectives
  Definition of an angular dependent secondary electron emission yield (SEEY) model
  Effect of the angular dependence of SEEY on the charging simulation
Method
  Measurement and modeling of incidence angle effect on SEEY
  Implantation of this new model in SPIS
  Assessment of the angular effect on a SPIS simulation

## Slide 3: TSEEY basics
EEY
Typical Electron emission yield (EEY*) curve shape
EEY max
E0 max
E0
Mean escape depth
*Called also SEY

## Slide 4: TSEY measurement
Incidence angle effect
Backscattered electrons yield
secondary electrons yield
T. Ginest et al, Meas. Sci. Technol. 25 (2014) 085601

## Slide 5: Measurement facility
Pressure 10-10 mbar in the analyse chamber and 10-7 mbar in the introduction chamber
3 electrons gun 1eV-2 keV, 50 eV – 5 keV and 1keV-22 keV
Ion source (25 eV -5 KeV)
Hemispherical electron energy analyser
Kr VUV lamp
Gaz analayser
Facraday cups
Electron colector
Manipulator X,Y,Z,
Working Temperature RT to 500°C
Incidence angle 0 to 90°
DEESSE
Energy analyser
gaz analyser
Ion gun
electron gun
@onera

## Slide 6: Model discrepancies (on silver)
Measurements
SPIS (and NASCAP) models
Discrepancies:
  Globally on the values
  But also on the behaviour and the waveform

## Slide 7: Model discrepancies (on silver)
Measurements
SPIS (and NASCAP) models
 Fitted at normal incidence
Discrepancies:
  Globally on the values
  But also on the behavior and the waveform
  Angle effect every time overestimated

## Slide 8: Dielectric measurements
50eV, 60°
Electron gun
Electron emission yield for dielectric samples (many possible artefacts due to the charging effect)
+
-
Incident energy > adjusted energy
recollection of secondaries
Deviation of the electron beam
Origine of chagrin
  Triboelectric effect (i.e: Teflon)
  During the measurement (charge trapping)
It is mandatory to control the charging level
(very short electron pulses, kelvin Probe, specific charge neutralization strategy)
=> apparent yield< real yield
=> apparent yield=1

## Slide 9: Measurement results
CMX
CFRP

## Slide 10: Model results for isotropic flux
CMX
CFRP

## Slide 11: Electrostatic behaviour simulation
Standard GEO telecom platform
ECSS worst case environment

## Slide 12: Reference simulation results
Absolute potential is -5100 V
CMX cover glasses charge positively with respect to the spacecraft ground due to strong electron emission under photon irradiation  inverted voltage gradient (IVG) situation / negative grounded conductors and positive differential voltage of dielectrics.
Maximum differential potential on solar cell cover glasses of +2100 V (> 500 V – ie ECSS)
OSR charge negatively because at shade  direct voltage gradient (DVG) / negative differential voltage of dielectrics
Secondary electron emission partly mitigates this situation
Important parameter  electric field within the thickness of the dielectrics 39 V/µm
Main ESD risk for the satellite thus comes from the solar panels.

## Slide 13: Surface potential evolution
Time (s)
Time (s)
Potential (V)
Standard
Dekker 60

## Slide 14: Surface potential evolution
Time (s)
Time (s)
Potential (V)
Standard
Standard fitted

## Slide 15: Secondary electrons density
Standard
Dekker 60

## Slide 16: Differential potential
Time (s)
Time (s)
Potential (V)
Standard
Dekker 60

## Slide 17: Conclusion
 | spacecraft ground | CMX max IVG
 | kV | kV
Reference case | -5.1 | 1,6
Dekker 90 | -3.2 | 1,0
Dekker 60 | -3,7 | 1,3
Reference with updated params | -5.1 | 1,8
Tacking a realistic angular dependency:
  Smaller effect of angle of incidence than predict in model
  Due to surface state effect no angular dependence at low energy
On the SC:
  Smaller emission from CMX
  Higher emission from CFRP
Smaller IVG than predicted in the standard model